Part Number:

0533980471

Status:

Active

Overview:

PicoBlade™

Description:

1.25mm (.049") Pitch PicoBlade™ Header, Surface Mount, Vertical, Lead-free, 4 Circuits

Documents: Note - Please disable browser pop-up blockers for documents on www.molex.com

- Drawing (PDF)

- Product Specification PS-51021-024 (PDF)

- 3D Model

- Related Catalog Page (PDF)

| General |
| --- |
| Product Family | PCB Headers |
| Series | 53398 |
| Application | Wire-to-Board |
| Overview | PicoBlade™ |
| Product Name | PicoBlade™ |
| Physical |
| Breakaway | No |
| Circuits (Loaded) | 4 |
| Circuits (maximum) | 4 |
| Color - Resin | Natural |
| Durability (mating cycles) min | 30 cycles |
| First Mate / Last Break | No |
| Flammability | 94V-0 |
| Guide to Mating Part | No |
| Keying to mating part | None |
| Lock to Mating Part | Yes |
| Mated Height Inches | 0.224 In |
| Mated Height mm | 5.70 mm |
| Material - Metal | Phosphor Bronze |
| Material - Plating Mating | Tin |
| Material - Plating Termination | Tin |
| Material - Resin | High Temperature Thermoplastic |
| Number of Rows | 1 |
| Orientation | Vertical |
| PC Tail Length (in) | 0.024 In |
| PC Tail Length (mm) | 0.60 mm |
| PCB Locator | No |
| PCB Retention | Yes |
| Packaging Type | Embossed Tape on Reel |
| Pitch - Mating Interface (in) | 0.049 In |
| Pitch - Mating Interface (mm) | 1.25 mm |
| Plating min: Mating (uin) | 40 |
| Plating min: Mating (um) | 1 |
| Plating min: Termination (uin) | 40 |
| Plating min: Termination (um) | 1 |
| Polarized to Mating Part | Yes |
| Polarized to PCB | Yes |
| Shrouded | Partial |
| Stackable | No |
| Temperature Range - Operating | -40°C to +85°C |
| Termination Interface: Style | Surface Mount |

| Electrical |
| --- |
| Current - Maximum | 1.000 Amp |
| UL | E29179 |
| Voltage - Maximum | 125V |